| TECHNICAL SPECIFICATION |
| --- |
| PART NO. | 4RF10008001001M1 |
| CABLE TYPE | NFC-100 COAXIAL CABLE |
| //STRUCTURE： |
| Conductor | /Composition(No./㎜) | 0.46mm |
|  | Material | Copper Cover Steel |
|  | Outside Diameter (㎜) | 0.46±0.008mm |
| Insulation | Material | Solid polyethylene (XLPE) |
|  | Thickness (㎜) | 0.52mm |
|  | Nom. Diameter(㎜) | 1.5±0.1mm |
| Shield | Material | Double Aluminum Foil |
|  | Construction | 0.038mm |
|  | Material | Tinned Copper Wire |
|  | Construction | 16*5/0.10mm |
|  | Picks/inch | 12 |
|  | Diameter(㎜) | 0.10±0.008mm |
| Jacket | Material | PVC (RoHS) |
|  | Diameter(㎜) | 2.8±0.10mm |
|  | Color | BLACK |

良泉公司

認可:

審核:

承辦:

| ELECTRICAL & PHYSICAL PROPERTIES |
| --- |
| PART NO. | 4RF10008001001M1 |
| CABLE TYPE | NFC-100 COAX CABLE |
| RATING TEMPERATURE & VOLTAGE | 60℃ , 30V |
| SPARK TEST | 3000V |
| INSULATION | UNAGED | TENSILE STRENGTH | 1500 PSI MIN |
|  |  | ELONGATION | 150 % |
|  | AGED | TENSILE STRENGTH | 70% ↑ |
|  |  | ELONGATION | 70% ↑ |
| JACKET | UNAGED | TENSILE STRENGTH | 1500 PSI MIN |
|  |  | ELONGATION | 100 % |
|  | AGED | TENSILE STRENGTH | 70% ↑ |
|  |  | ELONGATION | 65% ↑ |
| NOMINAL IMPEDENCE | 50 ± 3 OHM |
| NOMINAL CAPATCITANCE (pF/M) | 105 ± 3 |
| ATTENUATION | FREQUENCY (MHz) | dB/100M |
|  | 30 | 12.9 |
|  | 150 | 29.4 |
|  | 900 | 74.9 |
|  | 1800 | 109.0 |
|  | 2500 | 130.6 |
| 良泉公司 認可: 審核: 承辦: *以上衰減值公差+15% 續下頁 |
| ELECTRICAL & PHYSICAL PROPERTIES |
| ENVIRONMENT REQUIREMENT | EACH OF THE F,CI,Br,l,At Pb(ACCORDING/TO PA3050B) Cd(ACCORDING TO EN1122,2001) OTHER//HAZARDOUS//SUBSTANCES ARE CONFORM WITH SONY SS00259 AND ROHS ATANDARD |
| MARKING： |
| JACKET INSULATION ALUMINUM FOIL CONDUCTOR SHIELD |

環境相關聯物質一覽表

|  | SUBSTANCE NAME物質名稱 | CONIENT含量 |
| --- | --- | --- |
| Heavy Metals (重金屬) | Cadmium and cadmium compounds(鎘以及鎘化合物) | N.D |
|  | Lead and lead compounds(鉛以及鉛化合物) | N.D |
|  | Mercury and mercury compounds(汞以及汞化合物) | N.D |
|  | Hexavaient chromium compounds(六價鉻化合物) | N.D |
| Brominated Organic compounds (有機溴化合物) | Polybrominated biphenyls(PBB)(聚溴聯苯) | N.D |
|  | Polybrominated (PBDE)(聚溴二苯醚) | N.D |
|  | Other brominated organic compounds (其它有機溴化合物) | N.D |